ISSN  1999-8716

Diyala Journal

of Engineering Sciences

Printed in Iraq

Vol. 03 , No. 01 , pp. 79-89 , June 2010

STaTE SOME MECHANICAL PROPERTIES FOR Al- ALLOY WELDED BY SEAM WELDING TECHNIQUE

latfe  Y .Zedan 1, and Ahmed  F. Hassn 2

(1,2) Engineering College , Diyala University

(Received:6-6-2009 ; Accepted:22-3-2010)

ABSTRACT - The aim of  this paper was perpetrated lap joint  welding samples welded by seam welding method ,2014 heat treatable aluminum alloy ,the paper studied some groups at different variable welding ,welding time was studied  at electrode pressure 1,1.5 KN with thickness 1.5 mm and another group at 2 mm .after welding process shear strength ,Vickers hardness were tested at different variables.

The paper stated the best shearing strength at 1.5mm thickness with 45 KA welding current at 1.5 KN electrode pressure.  Increase 0.5 mm in thickness lead to decrease 20% of shearing strength.

KEY WORDS:- 2014 heat treatable aluminum alloy, seam welding, mechanical properties.

1- INTRODUCTION

Fusion welding, the joint is effected directly between the parts being joined by the application of heat to melt the interfaces and so cause the materials to fuse together. Fusion welding thus requires the melting point of the components to be exceeded.

There are four main types of process used for fusion welding.

- Electric arc.

- Electrical resistance

- Radiation

- Thermo  chemical.

The aluminum alloys and copper are difficult to weld because of the high thermal conductivity, high thermal expansion and a tendency to give porous welds(1).