ISSN  1999-8716

Diyala Journal

of Engineering Sciences

Printed in Iraq

Vol. 03 , No. 01, pp. 106-121 , June 2010

Mathematical and Quantum Chemical Studies for the Corrosion Inhibition of Steel in HCl Acid

Anees A. Khadom

Engineering College , Diyala University

(Received:9-12-2009 ; Accepted:7-4-2010)

ABSTRACT - The application of empirical and quantum chemical models on the corrosion inhibition of steel in hydrochloric acid in presence of phenylthiourea (PTU) as corrosion inhibitor have been modeled. Two mathematical models were used, third order polynomial model and Arrhenius type equation model. Levenberg-Marquardt method was used to evaluate the coefficients of two Models. Two models were suitable to represent the corrosion rate data at different conditions. The correlation coefficient of third order model was 0.973, while for the Arrhenius type model was 0.919. The structure of inhibitor was optimized by ArgusLab 4.0.1 package. The quantum chemical parameters (EHOMO, ELUMO, ΔE, and dipole moment µ) were estimated by PM3-SCF method.

KEY WORDS:- quantum chemical, corrosion inhibition, hydrochloric acid, carbon steel.

1- Introduction

Corrosion is a fundamental process playing an important role in economics and safety, particularly for metals and alloys. Steel has found wide application in a broad spectrum of industries and machinery; however its tendency to corrosion. The corrosion of steel is a fundamental academic and industrial concern that has received a considerable amount of attention (1). Using inhibitors is an important method of protecting materials against deterioration due to corrosion, especially in acidic media (2). Acid solutions are widely used in industry, some of the important fields of application being acid pickling of iron and steel, chemical cleaning and processing, ore production and oil well acidification. As acidic media, HCl and H2SO4 are generally used in the treatment of steel and ferrous alloys. Because of the